## Slide 1: BEARING LUBRICATION Best Practices 2/14/2024
Presenter – Dean Burcroff
Presents:

## Slide 2: BEARING LUBRICATION
Primary role
  Insert a oil film between all surfaces that are in rolling or sliding contact
Effects of Lubrication
  Reduces friction and wear
  Extends life of components
  Takes away heat from bearing
  Helps prevent contamination and guards against corrosion

## Slide 3: BEARING LUBRICATION Grease
Bearing grease is lubricating oil suspended in a thickening agent or base
Color is not a good indicator of grease type
Never mix greases with different bases
  See compatibility chart
PolyRex EM is the latest preferred Polyurea grease for electric motor bearings
Shielded/sealed bearings are lubed for life

## Slide 4: BEARING LUBRICATION Grease
Advantages
  Economical
  Overall cleanliness of the machinery
  Can act as a protective barrier
  Facilitates mountings
  Facilitates handling
  No external systems
  Simple, provides protection from contamination

## Slide 5: BEARING LUBRICATION Grease
Disadvantages
  Slower speeds than oil
  Friction torque higher than oil
  Lower cooling characteristics than oil
  Difficult to control volume of grease
  Not as easy to replace as oil
  Cannot remove particles from grease

## Slide 6: GREASE COMPATIBILITY CHART

## Slide 7: GREASE
Base oil in the grease provides the lubrication needed in an application
The thickener base of a grease is one of the most important factors when considering the mixing of grease
Common Additives
  Rust inhibitors
  EP agents
  Oxidation inhibitors
  Anti-wear agents

## Slide 8: BEARING LUBRICATION Grease Terminology
NLGI Rating published in 1938, adopted in 1941
  Consistency of lubricant
  #000 to #6
  #2 very common, consistency of Peanut Butter
Melting Point
  The point at which the grease is fluid enough to run
  Operable temperature is 100º F below melting point
Shear Stability
  Ability to withstand repeated working with a minimum change to consistency

## Slide 9: NLGI NUMBERING SYSTEM

## Slide 10: BEARING LUBRICATION Grease
Factors Affecting Grease Selection
  Operating speed
  Operating temperature
  Pressure
  Water Conditions
  Lubricating requirements of the other components in the system

## Slide 11: BEARING LUBRICATION Grease Fill
Ball bearings, 25-40%
Cylindrical roller, 20-30%
Mounted bearings, 50-100%
  Lubricate while running
Tapered roller bearings, 100%
IMPORTANT: Over-lubrication is as harmful as under lubricating
Do not add extra grease to quiet a bearing
  Allow grease time to evenly distribute throughout bearing
Volume of Grease - cm3
Ball Bearing Bore - mm

## Slide 12: BEARING LUBRICATION
Grease intervals will be different for different types of bearings
Self contained ball bearings are sealed for life and shouldn’t need re-lubrication (Most electric motors)
As load increases or less free space in a bearing, need for re-lubrication is more frequent

## Slide 13: BEARING LUBRICATION Grease Fill
Under Lubrication
  Boundary friction
  Lubricant starvation
  Increased wear
Over Lubrication, major cause of bearing failure
  Increase fluid friction
  Increase heat, which will oxidize grease
  Shorter operational life

## Slide 14: BEARING LUBRICATION
Effect of Fill Rate on Operating Temperature

## Slide 15: BEARING LUBRICATION
Properly packing a bearing with grease
Hand packing requires clean hands or gloves
Gauge proper fill based on fill charts
Generally smaller bearings contain higher fill rates than larger bearings when shipped by the manufacturer
Fill rate depends on speed, load, frequency of relubrication

## Slide 16: BEARING LUBRICATION
Lubrication Interval
Example: Ball bearing operating speed is 1,800 RPM. Limiting speed is 6,000 RPM
  Ratio 1800/6000 = 0.3
  Ball Bearing is 9,500 hrs
Roller bearings have lower limiting speed ratings than same sized ball bearings and require more frequent lubrication

## Slide 17: COMMON GREASES
Electric Motor greases
PolyRex EM
  Temp range -20 F to 350 F
  Polyurea
  More shear stable
PolyRex EP-2
  Temp range -20 F to 350 F
  Extreme Pressure
  Cylindrical Roller Bearings
Shell Alvania 2
  Temp range -30 F to 230 F
  Lithium base
Chevron SRI-2
  Temp range -20 F to 350 F
  Polyurea
  “Old standard” EM grease
No need to grease most electric motors

## Slide 18: TAPER ROLLER Grease Packing
When greasing bearing, pack either by hand or with mechanical bearing packer
  100% fill

## Slide 19: MOUNTED BEARINGS Lubrication Instructions
Most mounted units have a lithium base NLGI#2 grease as standard (Timken uses PolyRex EM=)
  Compatibility of grease must be assured
Follow recommended lubrication intervals
If safe, grease while running
  Pump in grease slowly until slight bead forms around seal
  A slight rise in temperature usually occurs
    10ºF to 30ºF is normal, temporary temp rise

## Slide 20: MOUNTED BEARINGS Lubrication Chart

## Slide 21: BEARING LUBRICATION Motorized Grease Gun
SKF TLGB 20/110V, battery powered
Follow all safety warnings and instructions
  20V DC lithium-ion rechargeable battery
    Battery and 110-120 v charger included
  LED light helps locate lubrication fittings
  LCD display shows battery charge, pump speed, and grease output
  Two grease output speeds 3.5oz/min or 5.5oz/min
  Grease capacity is 14.5oz
  Max pressure 10,000 psi
  6.5 lbs, 15 cartridges/charge

## Slide 22: BEARING LUBRICATION Automatic Lubricators
Advantages
  Proper metering of grease flow
  Stricter control over grease type
  Less waste
  Ensures continual lubrication
  Ensures hard-to-reach areas receive lube
  Reduces labor cost

## Slide 23: BEARING LUBRICATION Automatic Lubricators
Types
  Spring Operated
    Changing spring alters dispensing rate
    Reusable, refillable by grease gun
  Gas Operated
    Nitrogen or Hydrazine gas cartridge
    Allows for flow adjustment - 1 month to 2 years, based on plug used
    Throw away units

## Slide 24: BEARING LUBRICATION Automatic Lubricators
Types continued
  Battery / Motorized
    Dispenses at rate set by user
    Rates vary by unit and manufacturer
    Many have replaceable grease cartridges/batteries
    Multi-lubrication point units available
  Accessories available from most suppliers
    Lines, fittings, brushes, brackets, clamps, etc.

## Slide 25: TEMPERATURE OF BEARINGS
Most electric motors operate from 140-160 F
  Measure housing at bearing location to take temperature reading and add 15-20 F to estimate bearing temperature
Fan bearings may experience wide temperature variations because of environmental/season changes
In general, when grease is introduced, there will be a spike in temperature as the rolling elements push grease out of the way
  This could take 30 minutes to several hours

## Slide 26: IS THERE MOISTURE IN THE GREASE?

## Slide 27: WATER CONTAMINATION IN GREASE

## Slide 28: BEARING FAILURES

## Slide 29
Based on a study by an independent German insurance company, they found that only 0.5% of bearings actually fail due to overstressing of the steel.
B 20%
A
20%
C 15%
D 20%
E 5%
A
B
C
D
E
F
G
H
F 5%
G 5%
H 10%
I <1%
I
}
80% !
Liquid contamination
Solid contamination
Mounting faults
Secondary damages
Unsuitable choice of bearing
(design, size, load carrying capacitiy)
Insufficient lubricant
Aged lubricant
Material and production faults
Unsuitable lubricant
}
Source: Antriebstechnik 18 (1979) No. 3,
20%
CAUSES OF BEARING FAILURES

## Slide 30: PREMATURE BEARING FAILURES
Miscellaneous
  Electric current
  Design problem
  Material quality
Sealing deficiency
  Contamination
  Moisture
  Corrosion
Inadequate lubrication
  Lubricant shortage
  Improper lubricant
Improper Mounting
  Shaft or housing defect
  Misalignment
  Incorrect fits
  Excessive clearances
  Rough mounting
  Axial looseness
  Radial or thrust overload
  False Brinelling
  Contact corrosion
  Seal/Shield damage

## Slide 31: FLAKING OR SPALLING
Flaking at intervals on raceway
  Caused by impact load
Deep “Potholes” in outer ring raceway
Spalling in a ball bearing inner race

## Slide 32: BRINELLING
Is a sudden force that leaves dents or marks from the rolling element into a raceway
Bearing with brinelling will fail because of the damage
Causes
  Incorrect mounting forces
  Dropping bearing

## Slide 33: CONTAMINATION
Contaminants get into bearing from improper sealing, failure of seals, contaminated grease
  Can leave scoring, pitting, scratching
Water is another threat that will rust bearings
CONTAMINATION DAMAGE

## Slide 34: FAILURE BY HEAT EXPOSURE
Improper lubrication method or inappropriate lubricant
Can be preload, reverse loading, process heat or other causes
  Look for blue/black and silver/gold discoloration.
  Balls will usually be blue/black.

## Slide 35: MISALIGNMENT FAILURE
Caused by bent shafts
Shaft and housing not square
Shaft misalignment transferred through shaft into bearing
Can cause broken cage

## Slide 36: FRETTING CORROSION
Insufficient interference
Happens often in mounted bearings between the inner race and shaft

## Slide 37: WATER ETCHING
Water etch is when water is exposed to bearing and stains rolling surface
If left too long it will turn into pits and cause failure of bearing

## Slide 38: SMEARING
Surface initiated damage from excessive sliding or skewing between contact surfaces
Smearing wear on roller caused by contaminated lubricant

## Slide 39: CREEPING
Motion between the bearing ring and the mating part
  May appear as highly polished surface or discoloration
Insufficient interference
  Fitting selection should be reviewed and/or mating parts checked for wear

## Slide 40: FALSE BRINELLING
Vibration causes wearing while bearing is stationary
In storage, make sure bearings are not subject to vibration or isolate on vibration absorbent material

## Slide 41: CATASTROPHIC FAILURE
Seizure caused by chips on ribs
  Cause is excessive axial impact load
Cracks and chips
  Excessive axial impact load
Broken retainer
  Lubrication failure most likely cause

## Slide 42: BEARING DAMAGE FROM ELECTRICAL CURRENT
Electrical discharge machining (EDM)
  Electrical fluting / wash boarding
  Often found when VFD used on equipment

## Slide 43
BEARING PROTECTION FROM ELECTRICAL CURRENTS
=
Fixes: Aegis ring, ceramic coated ring, or ceramic ball

## Slide 44: BEARING SERVICE Premium Service, Expert Solutions
Thank You for your time!