## Slide 1: What to do about material contamination The easy material is gone
21st July 2023
Mark Krause | North America Managing Director

## Slide 2: As we continue to grow and expands two things are happening
Deposits with lignite, coal and other contaminants must be processed
Recycle Aggregates are coming into play
  In larger cities where material is now a larger haul distance to usage.

## Slide 3
Contaminant Removal

## Slide 4
1
2
5
3
6
8
11
8
10
12
13
7
Tk-101
P-101
FT-101
Scrn-101
Scrn-102
Tk-102
P-102
Cy-102
Process Water
Feed (-4mm )
To Ponds or
Water Treatment
Lignite / Coal
Free Sand
Lignite, Coal,
Light Materials, etc.
General Process Flow Diagram for Removal
of Lignite and Coal from Sand -- Conveyable Discharge
4
Cy-101

## Slide 5
Lignite in overflow is
removed by the sieve
bend.

## Slide 6
Organics
Feed
Fine
Sand
Coarse Sand
Sieve
Bend
FBC
Classifier
Flat Bottom Classifier: The “Heart”
of the System

## Slide 7
Classifier underflow and sieve bend underflow report to sand screw for dewatering
Lignite will drop into
catch basin
Lignite Removal From
Concrete Sand

## Slide 8
Feed topsize - 3/8”
Cut between 200 mesh & 35 mesh
Classification by Size

## Slide 9
Must be at least 0.7 SG difference in minerals
Can be problem if lighter mineral has much larger particle size
Separation by Density

## Slide 10
Common case of density separation - lignite SG 1.4 & Silica SG 2.7 difference = 1.3
Use with Sieve Bend on overflow to recover fine sand
Removal of Organics

## Slide 11
Tank
Weir
O/F Launder
Plenum
Chamber
Plate with
Nozzles
Plungers
Outlet Ports
Feedwell
Air Cylinders
Level Probe
Parts of a FBC

## Slide 12
Feed enters –
50 to 65% w/w
Teeter Water gives
a rising current
Teeter Bed Forms
Operation

## Slide 13
Teeter Water gives
a rising current
Teeter bed segregates
Fines to top
Coarse to bottom
Fines Overflow Weir…
..& exit Launder
When the Level Probe detects that the sand bed level reaches the setpoint
The Plungers open for ½ second to let out some coarse material
Operation

## Slide 14
For size classification at 140 Mesh capacity is 10 to 15 MTPH of dry solids per m².
The finer the cut size, the lower tph capacity for a given size of Classifier.
For size classification at 35 Mesh capacity is 35 to 40 TPH of dry solids per m².
Rules of Thumb

## Slide 15: Common Questions
What happens if the recommended loading rate is exceeded?
  Efficiency of size separation decreases
How much lignite is removed?
  Approximately 95% with a 50 mesh size separation

## Slide 16: Wet Recycling: EQUIPMENT LOOKS SIMILAR BUT PROCESS FLOW IS DIFFERENT

## Slide 17: DEFINITION OF AGGREGATES
Primary aggregates are naturally occurring deposits of minerals that come in the form of crushed rocks, sand and gravel
Recycled aggregates are the product of processing inert construction, demolition and excavation waste, asphalt millings and used railway ballasts into construction aggregates.
Secondary materials are derived from other industrial processes including: China clay / Fly Ash / Incinerator Bottom Ash / Blast furnace slag
Source MPA

## Slide 18: DEFINITION
WHAT ARE THE ENVIRONMENTAL DIFFERENCES?
The biggest difference between virgin and recycled aggregate is the impact on the environment. Virgin material needs to be mined, and this requires digging up land, using a variety of tools and equipment, and then processing the material for use. All of this can use valuable natural resources, cause pollution, and consume energy.
Since recycled aggregates are already coming from a previously existing product, they do not need to be mined for use. This allows companies to conserve the natural resources while also eliminating the need for products to take up space in a landfill.

## Slide 19: DEFINITION
WHAT ARE THE COST DIFFERENCES?
There are many factors that determine the cost of aggregate, and when comparing recycled vs. virgin aggregate, recycled is generally the more cost-effective option. Since companies don’t have to mine or produce new material, they can price the recycled material lower than the virgin material. Since recycled producers already have the raw material at their facility, costs are generally lower, and savings are passed on to the consumer.
In some instances, you may actually get more recycled material than virgin material for the same or a lower price. For example, recycled CA6 is 15% lighter than virgin CA6, so you receive 15% more volume per ton. All of this adds up to a significant cost savings.

## Slide 20
GENERAL MIX MATERIAL
General mix material contain of excavation, concrete, wood, plastic, etc.…

## Slide 21
RECYCLE FACTS
An average new home building project generates about four tons of debris, according to Yost. That includes two tons of wood debris, a ton of drywall, 1,000 pounds of masonry, 600 pounds of cardboard, 150 pounds vinyl and 150 pounds of metals.

## Slide 22: EQUIPMENT LOOKS SIMILAR BUT PROCESS FLOW IS DIFFERENT

## Slide 23: WASH PLANT CONFIGURATIONS FOR RECYCLED AGGREGATES
Wash plants for recycled aggregates are available in a variety of configurations from simple to extremely complex.
Tonnage
Products

## Slide 24: RECYCLED CONCRETE
Advantages of Recycled Concrete:
Delivers a low cost alternative to exhausting local natural raw aggregates.
Concrete constructed with crushed recycled concrete has a lower carbon footprint
Slows down depreasion of natural aggregates
Uses less energy than natural aggregates
Lowers construction cost.

## Slide 25: RECYCLED CONCRETE
Disadvantages of Recycled Concrete:
Produces a lower grade of concrete than all natural. Less durable
Workability of concrete can be affected
It has less compressive strength
Has not been spec’ed in all areas as of yet.

## Slide 26: Where can I find more information?

## Slide 27: Where can I find more information?

## Slide 28
THANK YOU